## Slide 1: AFRL materials genomics workshop An introduction to local exchange functionals and ACBN0

## Slide 12: Need of fast and accurate HT first principles methods
Need to move beyond the current paradigm of DFT-PBE for materials description
Necessary requirement to describe successfully novel materials with strong electron localization and correlation
Develop and implement novel theoretical methodologies and computational techniques to address the challenges of the high-throughput environment by striking a balance between controllable accuracy and computational efficiency
Techniques that can simultaneously address the localized (molecular) and delocalized (solid-state) electronic structure
Volume, Variety, Velocity, Veracity

## Slide 13: The PAO-3G basis set
The PAO basis functions can be directly fitted using linear combinations of spherical-harmonic Gaussian functions and eventually expressed as Cartesian Gaussians
Definition of a new localized basis set: PAO-3G – each PAO is fitted using three Gaussians – directly in the UPF format!

## Slide 14: Coulomb and Exchange Integrals
Density matrix
Known from the filtering+shifting procedure
Localized orbital formulation ➔ easy evaluation of two-electron integrals
Library of PAO-3G basis functions in the
pseudopotentials UPF format
Reformulation of exact-exchange functionals
Provides a simple and accurate connection between plane-waves solutions and a localized basis set of minimal dimensions
Direct calculation of Hartree-Fock energies:

## Slide 16: DFT+U
Use the Hubbard model to describe the most localized states of the system - correction of the mean-field delocalized nature of DFT
EDFT+U=EDFT+EU
EU form borrowed from Hartree-Fock energy – correction of the mean-field density-density electron correlation with a HF Hamiltonian
EDC – double counting term that has to be subtracted from the original EDFT
where

## Slide 17: DFT+U
Same spirit of the exact-exchange functionals where the XC part of the functional is shaped as a Fock operator on the KS states
Important differences!
Effective interactions in DFT+U are screened and not based on the bare Coulomb interaction as in HF
DFT+U acts on a subset of states of the system: typically the localized d and f orbitals
Severe problems!
The screened Coulomb potential is not known
Ambiguity in the computation of the critical parameters
Although procedures for the ab initio computation of U and J have been proposed (cRPA, cLDA, etc.) U and J are typically used as “fitting” parameters to reproduce the correct experimental electronic structure of the system

## Slide 18: DFT+U: the wish-list
The five criteria for a GOOD DFT+U functional:
W.E. Pickett, S.C. Erwin, and E.C. Ethridge, Phys. Rev. B 58, 1201 (1998)
(LDA)PBE +U, reduces to (LDA)PBE when (LDA)PBE is known to be good
the energy is given as a functional of the density
the method specifies how to obtain the local orbital in question
the definition of U and J is provided unambiguously
the method predicts antiferromagnetic insulators when appropriate and improves the description of highly correlated metals.

## Slide 19
The algorithm behind
AFLOWLIB v.2: ACBN0

## Slide 20: ACBN0: the ansatz
Consider the clean HF formulation with the bare Coulomb potential restricted to a single Hubbard site
The HF local energy is computed in the PAO local basis (2 electron integrals from PAO-3G) – without an explicit HF calculation!
U and J are computed directly on the chosen Hubbard center from the Coulomb and exchange Hartree-Fock energies of the solid introducing a reduced density matrix
  where is the Mulliken charge of the basis of the localized orbitals,
  and cμi are the projections of the KS solution on the PAO basis:
  effective renormalized occupations as weighting factors that specify the on-site occupation of each electronic state that comes directly from the solution of the KS Hamiltonian

## Slide 21: ACBN0: the ansatz
The effective on-site HF Hubbard energy is thus computed as
  where the two electron integrals are restricted to the the local set of Hubbard orbitals
The on-site energy requires the computation of a small number of electron-repulsion integrals, namely only those involving the {m} set (i.e. 54 integrals for the d shell)
The PAO-3G projection scheme allows the calculation of EHF for periodic solids via a simple generalization (no cluster or finite size calculations)
Pmm’ carries all the information of the electronic structure
of the system from which it is derived

## Slide 22: ACBN0: the ansatz
See also related works from A. Andriotis et al., PRB 2010 and E. Carter et al., J. Chem. Phys., 2008
From the direct comparison with the original Anisimov formula we derive the expression for U and J in the general case of a spin-polarized system
Pmm’ depends on the electron density, since it is derived from the PAO-3G projection scheme
IT IS A TRUE DENSITY FUNCTIONAL

## Slide 23: ACBN0: the algorithm
Simplified self consistent scheme for the solution of the KS-ACBN0 equations:
Initial U=0
First effective U from ACBN0
Back as a DFT+U calculation
Iterate until U (and total energy) are converged
Completely integrated in the AFLOW-𝞹 framework
ACBN0

## Slide 24: Transition Metal Oxides
Wide range of 3d shell fillings 3d2 , 3d5 , 3d8 , and 3d10 in Ti, Mn, Ni and Zn
Substantial correction wrt the PBE values
U and J calculated for both TM and oxygen – UO not negligible and essential for the correct representation of the electronic structure

## Slide 25: TMOs: TiO2
Converged values for the rutile environment are Ti U3d= 0.15 eV and O U2p= 7.34 eV
Focus on oxygen – potential implication for proper description of O vacancies in TiO2
Band gap increases from 1.98 eV (PBE) to 2.83 eV (ACBN0) vs. an experimental value around 3.3 ± 0.5 eV
Band width in agreement with many-body GW calculations

## Slide 26: Magnetic TMOs: MnO and NiO
Increase of the bandwidth of the occupied manifold, in agreement with experiments and many-body (GW) calculations
Increase of the t2g bonding-antibonding splitting across the bandgap and indirectly the separation of the 4s parabolic band (correction of the position of the conduction d bands in NiO!)
Increase of the band-gap (direct and indirect) and of the band-width
Excellent agreement for the total magnetization

## Slide 27: Magnetic TMOs: magnetic ordering in MnO
ACBN0 correctly predicts the stability of the antiferromagnetic insulator state of TMOs when appropriate
ACBN0 correctly predicts the stability of the antiferromagnetic insulator state of TMOs when appropriate

## Slide 28: Novel HT- enabling tools for accelerated materials replacement
Validation of the ACBN0 functional:
Zn and Cd oxichalcogenides
28

## Slide 29: ZnX and CdX oxides and chalcogenides (X=O,S,Se,Te) - electronic properties
wz
zb
rs

## Slide 30: Validation of ACBN0
Accuracy comparable with EXX functionals
and many-body calculations!!
AFLOWLIB v.2
AFLOWLIB v.1,
Materials Project.
AiiDA…
Accurate but
prohibitively
expensive
30

## Slide 31: Band structures
31

## Slide 32: Phonon dispersions
32

## Slide 33: ZnO – Theoretical Spectroscopy
Improvement is the electronic structure translates in improvement of other properties as well
Excellent agreement of phonon dispersion with experiments – thermal properties
PBE
ACBN0
33
FD subpackage in Phonon developed at UNT
Finite differences and finite fields

## Slide 34: ZnO – Theoretical Spectroscopy
experiment
theory (FF/FD)
T. Sander et. al. PRB 85, 165208 (2012)
34

## Slide 35: Convergence of Ueff
Excellent convergence in less that 5 iterations

## Slide 36: CdO - band structure
Within PBE, the system is a metal (indirect gap)
Cd U3d=11.3 eV and O U2p=3.9 eV give a direct band-gap of 1.98 eV (exp. 2.24 eV)
Good agreement with experiments for both the band gap and the position and width of the d bands

## Slide 37: GaN
Ga U3d=23.5 eV (full core d shell – atomic limit) and N U2p=4.2 eV give a band-gap of 3.8 eV slightly higher than experimental results (3.4 eV) - same as HSE
The high U value on Ga d affects only the position of the core levels and not the valence band behavior
In general, hybridization in semiconductor is important – sp, pd cross U terms

## Slide 38: Interfaces
Variation of U across the interface – influence on the band alignment

## Slide 39: ACBN0: the check-list
Back to the five criteria for a GOOD DFT+U functional:
(LDA)PBE +U, reduces to (LDA)PBE when (LDA)PBE is known to be good
When the localized bands are not readily disentangled from other bands or when the orbitals are not thoroughly well localized. In the latter case, the method yields proportionally lower values of U – for instance Si 2p states yield a value close to zero

## Slide 40: ACBN0: the check-list
Back to the five criteria for a GOOD DFT+U functional:
(LDA)PBE +U, reduces to (LDA)PBE when (LDA)PBE is known to be good
the energy is given as a functional of the density
The value of U in ACBN0 depends only on the electron density. The ACBN0 functional can be considered a zeroth-order pseudo-hybrid density functional in the sense that it includes an on-site form of the Hartree-Fock exchange

## Slide 41: ACBN0: the check-list
Back to the five criteria for a GOOD DFT+U functional:
(LDA)PBE +U, reduces to (LDA)PBE when (LDA)PBE is known to be good
the energy is given as a functional of the density
the method specifies how to obtain the local orbital in question
As seen above, there is no need to specify any orbital explicitly: even though the information of the expansion coefficients is conceptually included in the renormalized density matrix, they are not individually resolved.

## Slide 42: ACBN0: the check-list
Back to the five criteria for a GOOD DFT+U functional:
(LDA)PBE +U, reduces to (LDA)PBE when (LDA)PBE is known to be good
the energy is given as a functional of the density
the method specifies how to obtain the local orbital in question
the definition of U and J is provided unambiguously

## Slide 43: ACBN0: the check-list
Back to the five criteria for a GOOD DFT+U functional:
(LDA)PBE +U, reduces to (LDA)PBE when (LDA)PBE is known to be good
the energy is given as a functional of the density
the method specifies how to obtain the local orbital in question
the definition of U and J is provided unambiguously
the method predicts antiferromagnetic insulators when appropriate (and improves the description of highly correlated metals – in the works!!!).

## Slide 44: ACBN0: the check-list
All this at (almost) the price of a regular PBE+U calculation!!!